# INSTA-LAWN / BLUEGRASS

# Technical Data

| Property | Imperial Unit | Metric Unit | Description |
| --- | --- | --- | --- |
| Fiber Type |  |  | 100% Thiolon Polyethylene LSR |
| Fiber Mass | 8,000 denier slit film | 8800 d tex slit film |  |
| Pile Height * | 2.0 in | 50.8 mm |  |
| Color (s) |  |  | Evergreen |
| Tufting Gauge ** | 1/2 |  |  |
| Stitch Rate ** | 11 / 3 in. | 1.44 / cm |  |
| Primary Backing | 6.5 oz/yd² | 220 g/m² | Stabilized dual layered woven polypropylene |
| Secondary Backing | 8.5 oz/yd² | 288 g/m² | DuraFlo |
| Non Woven Scrim | 2.5 oz/yd² | 85 g/m² |  |
| Optional Secondary Min. footage required | 20.0 oz/yd² | 678 g/m² | Urethane-Scrapecoat with perforations |

| Property | Imperial Unit | Metric Unit | Test Method |
| --- | --- | --- | --- |
| Face Weight | 33.0 oz/yd² | 1119 g/m² | ASTM D418 |
| Total Weight, Dura Flo | 50.5 oz/yd² | 1712 g/m² | ASTM D418 |
| Total Weight, Urethane | 59.5 oz/yd² | 2017 g/m² | ASTM D418 |
| Permeability |  |  | DIN 18-035, part 6 |
| Tuft Bind | 9 lb - f | 40 n | ASTM D1335 |
| Grab Tear MD | 200 lb | 91 kg | ASTM D5034 |
| Grab Tear CMD | 200 lb | 91 kg | ASTM D5034 |
| Infill Amount, recommend | ¾ of Pile Height |  |  |

| Property | Imperial Unit | Metric Unit | Description |
| --- | --- | --- | --- |
| Item Number, Dura Flo |  |  | EL33 |
| Item Number, Urethane |  |  | XT33 optional |
| Roll Width | 15 ft. | 4.57 m |  |
| Roll Length *** | 100 ft. | 30.5 m |  |
| Area per Roll *** | 1500 ft.² | 139.4 m² |  |
| Total Roll Weight, Dura Flow | 526 lbs. | 239 kg |  |
| Total Roll Weight, Urethane | 619 lbs. | 281 kg |  |

# Text boxes

Product Properties

Performance Properties

Packaging